Supplemental Table 1. Protein quantification in the native and decellularized porcine jejunal segment.

|  | SicrolTM Soluble Collagen Assay* | BlyscanTM Sulfated GAG Assay* | FastinTM Elastin Assay* |
| --- | --- | --- | --- |
| Substrate | all collagen types | Proteoglycans, GAG | elastin |
| Composition | collagen type I, 0.5 M acidic acid | sulfated GAG, ovine chondroitin sulfate | ovine α-elastin, 0.25 M oxalic acid |
| Concentration | 1 mg/ml | 100 µg/ml | 1 mg/ml |
| Dilution (probe) | 1 : 10 | none |
| Dilution (pos. control) | 1 : 10 | none |
| Dilution (neg. control) | none |
| Probe volume | 100 µl |
| Dye | direct red 80 | dimethyl-methylen-blue (DMB) | porphin-5, 10, 15, 20-tetraphenyl-21,23-porphin tetra-sulfonat (TPPS) |
| Dye volume | 1 ml |
| Incubation | 60 min, horizontal shaker (200 rpm) | 90 min, horizontal shaker (1000 rpm) |
| Centrifugation | 10.000 rpm for 10 min |
| Complex solving reagent | 0.5 M sodium hydrate | chaotropic salts, propanol | guanidine-hydrochloride, propanol |
| Reagent volume | 1 ml | 350 µl |
| Incubation | 5 min horizontal shaker | 10 min horizontal shaker |
| Volume per well | 200 µl | 100 µl |
| Wave length | 540 nm | 656 nm | 513 nm |

* Biocolor, Newtownabbey, UK