Supplementary Table 1. Physiochemical properties of TAF+EVG NPs

| NP type | Particle size (nm) | Zeta Potential (mV) | PDI | % EE | % DL |
| --- | --- | --- | --- | --- | --- |
| TAF+EVG | 192.76 ｱ 12.4 | -20.74 ｱ 3.67 | 0.153 ｱ 0.018 | TAF: 54.1 ｱ 3.6 EVG: 44.6 ｱ 2.4 | TAF: 3.5 ｱ 1.1 EVG: 2.8 ｱ 0.79 |
| All data are presented as mean ｱ SE; n=5 independent TAF+EVG-NP batches % EE = percent entrapment efficiency; % DL = percent drug loading. |